## Slide 1
Increase in Performance of Static Seals
with innovative gasket products from FRENZELIT
Dipl.-Ing. Peter Übelmesser
Senior Manager Key Account Chemistry
Frenzelit GmbH

## Slide 2: Frenzelit GmbH, Bad Berneck (D)
  480 employees globally
  turnover ~ 90 Mio. €

## Slide 3
R&D
material production
application engineering
gasket production + logistics
FRENZELIT
partner
Supply chain competence

## Slide 4: Our product range
Gaskets
Technical Textiles
Expansion Joints
Insulation
New Materials

## Slide 5
Fluoropolymer
Aktive fillers
Aramid fibers
Glass fibers
Aktive filler
Various binders
Expanded graphite
purity > 99%
Stainless steel reinforcement (AISI 316 L)
- Expanded metal
- Steelfoil
Aramid fibers
Functional fillers of graphite
Mica
Stainless steel AISI 316 L
High efficiency binders
PTFE-gasket material
novaflon®
Elastomere-bound fiber gasket
novapress®
Graphite gasket
material
novaphit®
Engineered graphite with Kevlar®
novatec®
Mica based gasket material
novamica®
up to 260 °C
up to 83 bar
up to 200 °C
up to 100 bar
up to 550 °C
up to 250 bar
up to 300 °C
up to 100 bar
up to 1000 °C
60 bar
Material Competence in Gasket Materials

## Slide 6
novaphit® SSTCTA-L
novaphit® MST
Reinforced with expanded metal (1.4404)
High performing expanded graphite
Additional performance by XP-Technology
Increase in Performance of novaphit® by XP-Technologie

## Slide 7
Close-up of Tanged Metal Insert

## Slide 8
Weak Point Tanged Metal – Danger of Flange Deformation

## Slide 9
Weak Point Tanged Metal – Danger of Flange Deformation

## Slide 10
Flangedeformation caused by Gaskets
 Example: Tanged Metal as Metallic Reinforcement
Metallic Reinforcement

## Slide 11
Flangedeformation by Camprofil Gaskets
Metallic Reinforcement

## Slide 12
flangedeformation by camprofil gaskets - practical example
Damage caused by metal camprofile

## Slide 13
novaphit® - Technology
Expanded Metal as Closeup View
Metallic Reinforcement

## Slide 14
tanged metal:
Expanded metal:
Pi
Pi
Working Principle of Reinforcing Structures
Gasket thickness 2mm, Q=30 N/mm², sensitivity: medium
Metallic Reinforcement

## Slide 15
Chart: Mass-loss of Different Graphite Films Cgraphite = 99 %
| 300 | 350 | 400 | 450 | 500 | 550 | 600
Hochwertige Graphitqualität | 0 | 0.0625 | 0.125 | 0.25 | 0.5 | 0.75 | 1
Standard Graphitqualität | 0 | 0.5 | 1 | 3 | 10 | 22 | 44
No Name Graphitqualität | 0 | 1 | 3 | 10 | 22 | 51 | 100
High Performing Graphite
TGA Netzsch 209 IRIS
80% N2; 20% O2
time: 8h

## Slide 16
    Oxidations of Graphite Films in Molten Salt of
    KNO3 at 350°C
high performing graphite film
no name graphite film
day 1
day 3
day 30
day 60
day 96
High Performing Graphite

## Slide 17: What is the Practical Influence of Mass-Loss by Oxidation?
Chart: 
C: No Name Grafitfolie 99% | 0.063 | 0.117 | 0.144 | 0.166 | 0.205 | 0.304 | 0.327 | 0.376 | 0.507 | 100
High Performing Graphite

## Slide 18: Is there any Improvement?
XP-Technology

## Slide 19
Enhanced Stability against Oxidation by XP-Technology
Mass-loss by oxidation acc. to DIN 28090-2, TGA at 670°C/h
graphite purity 99%
XP-Technology

## Slide 20: What Else?
XP-Technology eliminates one principle weakness of Graphite
Have a look…
XP-Technology

## Slide 21
48 h @ 300°C
@ 30 MPa
air
Conventional Graphite Gaskets
XP-Technology

## Slide 22
Conventional Graphite Gaskets
(Power Plant of Chemical Production Site)

## Slide 23
Time intensive dismounting of gaskets
Danger of damaging flanges
XP-Technology
Conventional Graphite Gaskets

## Slide 24
48 h @ 300°C
@ 30 MPa
air
novaphit® with XP – Technology
XP-Technology

## Slide 25
Easy cleaning of flanges
Low risk of damaging flanges
novaphit® with XP – Technology
XP-Technology
Notes: Normally, residues are easy to brush off

## Slide 26
XP- technology for novaphit®
principle of action
HL Zhang et al., Carbon 44 (2006) 2212–2218.

## Slide 27
Pump: L2NG-106/180-AHMKVI-G
Medium: Vaccuum Residue und Heavy Fuel Oil
Gasket: novaphit® SSTC TA-L with XP Technology (46)
Design Temperature: 260°C
Design Pressure: 10 bar
Leistritz Pumpen GmbH
XP-Technology

## Slide 28
Type: L2NG-220/125-AHMKRA-G
Medium: Bitumen
Gasket: novaphit® SSTC TA-L with XP - Technology
Design Temperature: 270°C
Design Pressure: 16 bar
Leistritz Pumpen GmbH
XP-Technology

## Slide 29
Typ of pump: magnetic clutch
Medium: Dowtherm RP
Max. temperature: 350°C Pressure: 16 bar Type of gasket: originally novaphit® VS Width: 4mm Leakage after 6 month
Optimized construction with increased number of bolts
New gasket type: novaphit® SSTC TA-L with XP -Technology Width: 6mm > 12 months without leakage
XP-Technology

## Slide 30: Summary novaphit® with XP-Technology
Works in the complete temperature and media range of graphite gaskets
No damage of flanges caused by not recommended metallic reinforcement (tanged metal)
No risk of damaged flanges by simplified cleaning processes (XP-Technology)
Reduced maintenance costs by quicker dismounting of gaskets (XP-Technology)
Increased longterm performance (XP-Technologie)
XP-Technology

## Slide 31
novapress® 880
Increase in Performance at NBR/Ar Gaskets
Notes: 14
Entwicklungssprung 1: bislang unerreichte 13555-Kennwerte
Entwicklungssprung 2: signifikant verbesserte Anpassungsfähigkeit bei gleichzeitig immer noch sehr guter Mechanik unter Temperatur
Weltneuheit: Gasket Code Technology

## Slide 32
Forderung aus VCI-Leitfaden
Qmin bei 40 bar max. 30 MPa
QSmin bei QA 30 MPa max. 10 MPa
Notes: 14
Die beiden Punkte zeigen wichtige Eckdaten, die von modernen Dichtungen erfüllt werden müssen, wenn man sie gemäß VCI-Leitfaden (Verband der Chemischen Industrie) einsetzen will. Dieser Leitfaden erleichtert die Umsetzung der TA Luft für Norm-Dichtungen – also Rohrleitungen. Es muss nicht jeder Flansch berechnet werden, wenn die Dichtungen die Anforderungen des VCI-Leitfadens erfüllen.
Der grüne Punkt (Qmin) stellt die FP dar, bei der die Dichtung die Leckageklasse L0,01 bei der Montage erreicht.
Der blaue Punkt (Qsmin) bezieht sich auf die Entlastungskurven (der Übersichtlichkeit wegen im Diagramm hier nicht gezeigt) – also die minimale FP im Betrieb, bei der Dichtheit L0,01 noch gehalten wird.
Für Laien empfiehlt es sich hier, eine fiktive Belastungskurven und die dazugehörige Entlastungskurve per Pointer anzudeuten.

## Slide 33
Chart: Leakage curve 40 bar
| 9.3333333333333339 | 14 | 25.666666666666668 | 39.333333333333336 | 55.333333333333336
classic fibre gasket | 1 | 0.1 | 0.01 | 0.001 | 0.0001
classic fibre gasket inner eyelet 0,1mm | 1 | 0.1 | 0.01 | 0.001 | 0.0001 | 1e-05
novapress 880 | 1 | 0.1 | 0.01 | 0.001 | 0.0001
novapress 880 inner eyelet 0,1mm | 1 | 0.1 | 0.01 | 0.001 | 0.0001 | 1e-05
Entlastung kl. FA | 0.005 | 0.008 | 0.02 | 0.04
Entl. 880 | 0.0005 | 0.0008 | 0.0025 | 0.009
Notes: 14

## Slide 34
Extreme Adaptability
Surface pressure 20 MPa, gasket thickness 2 mm
competitors classic
fibre gasket
novapress 880
Compressibility ASTM F36J:
6 %
Compressibility ASTM F36J:
18 %
Notes: 14

## Slide 36
Leakage by
Corrosion and Elution

## Slide 37
Leakage by
Corrosion and Elution

## Slide 38
New Material novapress® 880 – Original Shape of Gasket
Result:
less leakage
But:
Not yet tight!

## Slide 40
old shape
Aa = 416.489mm²
Qa = 30MPa
New shape
An = 229.643mm²
Qn = 54 Mpa
Qn/Qa = 1,81
An/Aa = 0,55

## Slide 41
Optimized Shape
Result:
Ready for Serial Production

## Slide 42
Damage and indentations
on an internal diffusor-plate
In this example a pit up to 0,3mm without flange revision is compensated by novapress® 880 (2mm)

## Slide 43: Summary NBR/Ar gaskets novapress® 880
Less machining of flanges and therefore increase of availability factors by increased adaptability of gasket material
Less corrosion on flanges and therefore less leakage due to increased adaptability of novapress® 880
Improved process safety during installation of the gasket due to increased forgiveness against flange damages or residues
Optimized shape of gaskets offers additional potential for safe flange connections

## Slide 44
Annahmen für BASF LU: |  |  |  |  |  | 
zu öffnende Flanschverbindungen/a | 600000 |  |  |  |  | 
Revisionszeitraum | 3…5 Jahre |  |  |  |  | 
Gesamtzahl Flansche/LU | 1800000 |  |  |  |  | 
Anteil FA in den Flanschen [%] | 10 |  |  |  |  | 
Anzahl FA in Stck | 180000 |  |  |  |  | 
davon mit IB [%] | 30 |  |  |  |  | 
Anzahl FA mit IB in Stck | 54000 |  |  |  |  | 
davon ohne IB [%] | 70 |  |  |  |  | 
Anzahl FA ohne IB in Stck | 126000 |  |  |  |  | 
 | novapress 880 |  |  | klassische FA Dichtung |  | 
 | DN25PN40 | DN80PN40 | DN300PN40 | DN25PN40 | DN80PN40 | DN300PN40
Anteil [%] an den FA Dichtungen | 30 | 40 | 30 | 30 | 40 | 30
Anzahl FA Dichtungen mit IB in LU | 16200 | 21600 | 16200 | 16200 | 21600 | 16200
Anzahl FA Dichtungen ohne IB in LU | 37800 | 50400 | 37800 | 37800 | 50400 | 37800
Leckage [kg] im Betriebszustand für FA mit IB | 82 | 170 | 118 | 9822 | 4858 | 11192
Leckage [kg] im Betriebszustand für FA ohne IB | 191 | 397 | 275 | 5730 | 5384 | 12370
Gesamte Leckage in Kg/a je Abmessung | 273 | 567 | 393 | 15552 | 10242 | 23562
Gesamte Leckage in LU in kg/a | 1233 |  |  | 49356 |  | 

## Slide 45
World debut: Gasket-Code-Technology
Notes: 14

## Slide 46
World debut: Gasket-Code-Technology
Traceability of each individual gasket regarding:
Material name
Production batch
Manufacturing period
Upon delivery (incoming goods inspection, quality assurance)
After dismounting (chemical and thermal stability)
„Industry 4.0“
Notes: 14

## Slide 47
novapress® 880
novapress® 880 is latest state of the art and most modern FA gasket
Allows TA-Luft conforming design of flange connection systems acc to DIN 1591-1 / VDI 2290
Signifcantly improved „fitness for purpose“ due to increased adaptability (ca. 3-x !!!)
Reduced risk of leakage even with problems of flange assembly and torque
Sustainable reduction of fugitive emissions
Economic advantages due to significantly higher performance
Applicable for a wide range of media e.g. for natural gases, drinking water, chlorine, food etc. with option of standardization
Notes: 14

## Slide 48
novapress® 880
Secure compliance with the VCI-criteria
Secure seal designs acc. to DIN 1591-1 / VDI 2290
Higher safety level thanks to lower leakage rate even in case of low surface pressure
Only one material for gaskets with or without eyelet („one fits all“)
Higher tolerance to flange uneveness thanks to higher adaptability (3x more !!!)
More safety thanks to traceability of cut gaskets
Economic advantages due to significantly higher performance
Notes: 14

## Slide 49
Modern gasket materials show significant increase in sealing performance!
Test us!
Resumee